Request Title: Request approve of negative photoresist ‘NR9-3000PY’ in SNF.

Requestor: 	Ji Won Seo			Date:  2020/01/06

Non-SNF staff, please complete the following:

Badger ID:	jwonseo@stanford.edu

Company name/PI:  Stanford university / Tom Soh

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material.  Negative photoresist NR26-12000PY, I attach the MSDS of the chemical in email.

- Vendor/manufacturer info: Futurrex Inc.,

Address: Corporate Headquarters, 24 Munsonhurst Road, Franklin, NJ 07416, USA

Phone number: 888-999-4188

Website URL: https://futurrex.com/en

- Reason for request: Firstly, I attach the protocol of NR26-12000PY, latest version.

Few months ago, I got an access for almost same material “NR9-3000PY” in SNF and am using now.

This NR26-12000PY make a photoresist film thicker compared to NR9-3000PY.

When I was in my previous lab, We always used the NR9 series for negative photoresist. It was very common negative photoresist.

The negative photoresist acted as a lift off sacrificial layer for metal pattern.

In SNF, there is a AZ5214IR  negative photoresist. However, the AZ5214 have very poor resolution and complicated process for patterning.

Moreover, there is a lol and lor series in SNF for lift-off process. However, they have too thin thickness of film and are not easy to be patterned by Karlsuss mask aligner.

Those are the reason for request this NR9-3000PY negative photoresist.

- Process Flow:

  - 4 inch Si wafer is spin-coated using Headway 2 or Headway 3, soft bake 150c for 3 min in hot plate near the Headway 2.

The reason why I would not use a hot plate in Headway 3 is because a temperature of the hot plate is not correct. And also, there is also a distance between Headway 2 and a hot plate near the Headway 2, which means many people are conducting solvent exposure during moving their sample from Headway 2 to the hot plate near the Headway 2.  So, a process that moving sample from Headway 3 to the hot plate near the Headway 2 is reasonable.

  - Exposure using Karlsuss 1 or 2 and my photomask for 50s

  - Post exposure bake, 115c for 1min using a hot plate near Headway 2

  - Development using Developer MF26A for 30s in wbmiscres developer bench.

  - After process, the NR9 photoresist can be removed by remover PG or acetone for 1min.

- Amount and form. One 16 oz. bottle. It is liquid.  I don’t need to mix it to use it.

- Storage: I will store my chemical at SNF. terial at SNF? Storage groups is L

- Disposal: The waste during spin-coating will be in zip-rock bag and disposed in resist-waste trash can.   Unused product is a RCRA hazardous waste with numbers U057 and D001.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: