Request Title:  Ion gel encapsulation in MVD

Requestor: 	Yaakov Tuchman				Date:  March 2, 2020

Non-SNF staff, please complete the following:

Badger ID:		ytuchman

Company name/PI: Alberto Salleo

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

This request is an extension of the process developed and approved in the PROM request “EIM-TFSI/p(VDF-HFP) Ion gel processing” approved on April 11, 2019.  Briefly, the multi-layer stack is composed of a semiconducting polymer, followed by a solid electrolyte layer, a second semiconducting polymer layer and a metal cap.  This request primarily concerns the processing of the electrolyte layer, of which there may be two variants; neither variant will be made in the fab.

- An ion gel layer consisting of the ionic liquid 1-Ethylimidazolium bis(trifluoromethylsulfonyl)imide (CAS# 353239-10-8) and poly(vinylidene fluoride-co-hexafluoropropylene) (CAS# 9011-17-0).  The gel is formed by mixing the two ingredients (EIM-TFSI and p(VDF-HFP)) in an 80/20 w% ratio and subsequently dissolving the mixed powder in Acetone.  We do not intend to form the gel layer in SNF, only to process it. Consequently, we expect that there will be no remaining solvent in the gel by the time the substrates would be introduced into the fab.

- A solid electrolyte layer consisting of a thin HDPCVD oxide which is then subsequently coated with an ionic liquid, 1-Ethylimidazolium bis(trifluoromethylsulfonyl)imide, for example.

- Vendor/manufacturer info: address and phone number, website URL.

EIM-TFSI:

Ionic Liquids Technologies GmbH

Salzstrasse 184

D – 74076 Heilbronn

Germany

Telephone +49 (0)7131-89839-0

msds@iolitec.de

https://iolitec.de/en

p(VDF-HFP):

Sigma-Aldrich

3050 Spruce Street

SAINT LOUIS MO 63103

USA

Telephone +1 800-325-5832

https://www.sigmaaldrich.com/united-states.html

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

Previous experimentation indicates that over time, the ionic liquid may migrate out of the p(VDF-HFP) matrix into the encapsulating HDPCVD.  Consequently, we require a barrier layer to protect between the device stack and the surrounding encapsulant.

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that f the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

As mentioned above, this request is an extension of an existing process flow.  The interested reader can refer to the referenced PROM request for more background.  In terms of the referenced process flow, we propose the following between steps 5 and 6:

  - Conformal ALD coating of Al2O3 or similar using MVD.  The ozone attachment allows for the chamber to be cleaned after the coating to counteract any potential residual polymer contamination.

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

The materials to be processed would be brought in as films of several hundred nanometers thick.

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

N/A

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

N/A

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: