Request Title:  	LaCoO3 (LCO) thin films on Al2O3 and LaAlO3 (LAO) substrates into SNF

Requestor: 		Mahnaz Islam					Date:  11/30/2020

Non-SNF staff, please complete the following:

Badger ID:	mzislam

Company name/PI:  Prof. Eric Pop

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or material. The material is thin film (thicknesses ranging from ~50 to 150 nm) of lanthanum cobaltite (CAS No. 12016-86-3) on either Sapphire or Lanthanum Aluminate substrates. The material is sputtered by collaborators at 700C, so a specific MSDS is not available. However, related MSDS are available for the powder form and the target. To be clear, this target was not used by our collaborators to sputter the films, rather La and Co targets were used in an Oxygen environment.

- Vendor/manufacturer info: The thin films were sputtered at 700C by our collaborators at Northrop Grumman Corporation.

- Reason for request: My aim is to make two-terminal lateral devices out of these films and study the electrical switching behavior of this insulator-metal-transition (IMT) oxides.

- Process Flow: This material will not be in any clean equipment groups. The process flow should be similar to Stephanie Bohaichuk’s (sbohaich), who has previously worked on IMT oxides such as VO2 and NbO2 in SNF.

LCO Channel definition

Headway spincoater –SPR 3612 or SPR220-3 (thickness to use needs to be determined), bake in nearby hotplate (temperature and time needs to be determined).

Heidelberg 1 or 2 – exposure (dosage and time needs to be determined), post exposure bake in nearby hotplate

Headway bench - MF-26A developer

Pt-mtl – etch LCO (etch recipe needs to be determined)

Wbflexsolv or outside of SNF - Photoresist will be removed with acetone

Contact pad

Headway spincoater– LOL 2000, bake, SPR 3612, bake.

Heidelberg 1 or 2 – exposure for patterning contact pads, bake

Headway bench - MF-26A

AJA evaporator or outside of SNF – Pd followed by Au evaporated

(Remover PG soak for lift-off– non-SNF lab)

- Amount and form. Thin films (~50 to 150 nm) deposited on Sapphire and LAO substrates

- Storage: These will be stored outside of SNF in a nitrogen atmosphere to minimize oxidation.

- Disposal: Etched-off contents will be disposed off in the standard manner.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: