Process or Materials Review Request Form

Request Title:    PVA Spin-coat and Strip

Requestor:     Gregory Pitner                                           Date:  1/23/2020

Non-SNF staff, please complete the following:

Badger ID:    gpitner@tsmc.com

Company name/PI: TSMC

Send completed form to: snf-promcommittee@lists.stanford.edu

Note: Details in this PROM committee request not for public release or discussion, only for safety review.

- The chemical or material. Please provide all common names, trade names, and CAS numbers where appropriate. Include an MSDS, if available; or provide the reason, if not. Make sure to include information for any new secondary chemicals (such as a developer for a new resist). Read the MSDSs as well as the Stanford Chemical Storage Groups to determine the Storage Group Identifier and Main Hazard Class of your chemical/material.

Poly (Vinyl alcohol) = PVA

Diluted in DI water at various concentrations between 1% and 20%

MSDS attached to email.

- Vendor/manufacturer info: address and phone number, website URL.

PVA is purchased from Sigma Aldrich part number 363073.

https://www.sigmaaldrich.com/catalog/product/aldrich/363073?lang=en&region=US

- Reason for request: Please give serious thought to this. If you have any process information (application notes from the vendor, protocol from another lab, experimental methods section of an article), please include it, preferably as attachments. Ask yourself these questions: Is this the latest procedure? Are there newer/safer alternatives that will also work for my project? Will any of the current SNF approved chemicals and materials work for me?

PVA is a water-soluble sacrificial layer useful for transfer of 1D and 2D materials, already in use in other areas of Stanford University. It can be drop-cast and spun-coated, used for transfer, then removed by a water soak. It is better than sacrificial metal films due to its cleanliness and additionally does require a plasma pretreatment to adhere to target wafers. PVA is non-hazardous in every way, and is similar to the material used in vinyl gloves but in a form that is soluble in water.

- Process Flow: Please provide a detailed process flow description on how and where you proposed to use this chemical. This should include all Lab equipment to be used for processing your wafers once your new chemical or material has been used (even if your new material is a film that is removed, it may still pose potential contamination concerns.) Make sure to include wet benches. Please note that if the chemical/material is to be used in any the "clean" equipment, purity specifications will be needed. This is most important for chemicals/material that are not normally used for VLSI device fabrication. To be allowed into a "clean" tool, the material should MOS grade or better.

Detailed process flow is described here:

- Start with pre-mixed 1%-10% weight poly-vinyl alcohol (PVA) in DI water.

- At Headway, use pipette drop-cast PVA onto chips >1 cm2 in size. Wait several moments before spinning at low speed to remove excess PVA.

- Bake on hotplate in litho area coated by Al foil at 60C for several minutes

- At any clean table surface, (e.g. near FirstNano CNT furnace) transfer PVA film to target substrate using thermal release tape, similar to transfer CNT processes using gold reported elsewhere [Nishant Patil, et al, IEEE Transactions on Nanotechnology, 2009]

- Remove PVA in DI water heated to 60C  at  WB Flexcorr using personal beaker.

- Dispose of DI water with PVA down AWN drain.

  - NOTE: If desired, waste can alternatively be collected for EHS in waste bottles. OR  beakers can be poured into solvent waste at WB Solvent.

- Amount and form. How much will you bring in? Is it solid, powder or liquid? (Note: as a general rule, powders are not permitted in the cleanroom.) Do you need to mix it to use it?

I would bring in < 100 mL of PVA diluted in DI water.

- Storage: Will you be storing your chemical/material at SNF? If so, please note any potential reactivity’s (this should be on the MSDS). Storage groups A, B, D and L are stored in the yellow solvent cabinet in the furnace support area, while storage groups C, E, F and G are stored on top of one of the Pass-through Carts. Ensure your chemical container or material is properly labeled. If there is no available room, it must be stored by in the bulk storage area. You will then need to obtain it from receiving area personnel each time you want to use it and return it to them when you are finished using it (or each time you leave the lab). Note that there is no storage of chemicals/materials in the processing lab or at any wet bench.

I would not store in SNF, but would store in my toolbox and transport into SNF through the rear service entrance each day it is used.

- Disposal: How will you dispose of any waste or excess chemical or material? In your discussions with experts and vendors, try to determine the best way to dispose of your spent chemicals and by-products. Please refer to the SNF Lab members Safety Manual for the different methods of waste disposal that are available in the lab.

Dispose of DI water with PVA down AWN drain. NOTE: If desired, waste can alternatively be collected for EHS in waste bottles, or DI water beakers can be poured into solvent waste at WB Solvent.

Dispose of aluminum foil from Headway in flammable waste bin wrapped in ziplock bag according to standard procedure for discarding excess resists spun at headway.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date:

V1.0