Request Title:  EKC-270 Protocol

Requestor:	Gary Yama						Date: 10/22/2020

Non-SNF staff, please complete the following:

Badger ID: gyama.snf@gmail.com

Company name/PI:

Send completed form to: snf-promcommittee@lists.stanford.edu

1. Name:  Dupont EKC-270 Plasmasolv Post-Etch Residue Remover, 2-(2-Aminoethoxy)ethanol (75%), Hydroxylamine (15.0%), Pyrocatechol (9.94%))

Storage group is L (flammables, combustables and organic solvents)

2. Vendor/manufacturer info: Vendor: EKC Technology, Inc.

2520 Barrington Ct., Hayward, CA  94545-1188

(510) 784-9105

Web URL https://www.dupont.com/products/aluminum-perr.html

3. Reason for request:

Removal of post etch residue, while minimizing underlying Ti layer etching.

This has been difficult to remove using heated ashing.

4. Process Flow:

i) Reserve both wbflexcorr 3 and 4. Activate wbflexcorr 3. (While working

with EKC-270, other people can not work aside)

ii) Obtain and label a waste container.

iii) Fill blue “in-use hazardous chemical” tags

iv) Fill a beaker with EKC-270, and place a thermometer into the beaker.

v) Slowly heat up this beaker on the hotplate to 65 ~75 degree C. (Monitor

the temperature with the thermometer, and stir the liquid frequently.)

vi) Load the wafers into a cassette.

vii) Dip the cassette into the heated EKC-270 solution. Let the samples soak in

EKC-270 for 30min.

viii) Prepare three beakers of DI water

ix) Dip the cassette up and down inside the first DI water 5 times

x) Repeat last step with the other 2 DI beakers.

xi) Place the last DI beaker under running DI water, and let it overflow for 5

min.

xii) Dry the samples with N2 gun.

xiii) Collect EKC-270 waste with the waste bottle. Fully rinse all beakers,

thermometer, and the cassette, Collect the rinsed DI water with the waste

bottle if it is colored.

xiv) Place the waste bottle in room 162A

- Amount and form. Will bring one gallon of liquid EKC-270.  Do not need to mix or dilute.

- Storage: Storage group is L (flammables, combustables and organic solvents)

are stored in the yellow solvent cabinet in the furnace support area.

7	Disposal: Collect EKC-270 waste with the waste bottle. Fully rinse all beakers,

thermometer, and the cassette, Collect the rinsed DI water with the waste

bottle if it is colored.  Place the waste bottle in room 162A .

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: