Request Title:  Extended Exposure ALD of Platinum in Savannah Systems

Requestor: 	Donald Gardner					Date:  3/20/2020

Non-SNF staff, please complete the following:

Badger ID:	don.gardner

Company name/PI: vqResearch / Chris Piercy

Send completed form to: snf-promcommittee@lists.stanford.edu

- The chemical or materials:

  - Barium titanate (BaTiO3) powder (<100 nm particle size)

Material: 		Barium titanate

Appearance:	White powder

Formula:		BaTiO3

Synonym:		Barium titanium trioxide

Molecular Weight:233.19 g/mol

CAS number:	12047-27-7

EC number:	234-975-0

  - Polyvinylidene fluoride (PVDF) powder

Material: 		Poly(vinylidene fluoride)

Appearance:	White powder

Formula:		(C2H2F2)x-

Molecular Weight:~534,000 g/mol

CAS number:	24937-79-9

  - N,N-Dimethylformamide solvent (DMF)

- Vendor/manufacturer info:

  - BaTiO3 powder from

TPL, Inc.
3921 Academy Parkway North NE

Albuquerque, NM 87109

(505) 344-6744

  - PVDF powder from Sigma-Aldrich, St. Louis, MO

  - DMF solvent from OmniSolv, McLean, VA

- Reason for request:

- We would like to sinter BaTiO3 thick films using barium titanite powder mixed into PVDF.  We plan to form and sinter a bulk BaTiO3 ceramic using paste extrusion for use as a dielectric for our DARPA-funded research project.

- This process has been demonstrated in the literature, see citation below.

Kim et al., Fabrication of Bulk Piezoelectric and Dielectric BaTiO3 Ceramics Using Paste Extrusion 3D Printing Technique, J Am Ceram Soc. pp 1-10, 2018;00:1–10. https://doi.org/10.1111/jace.16242

- Process Flow:

- The process uses powders, so the process will be done in room 155 (Mavericks)

- PVDF powder is first dissolved in DMF solvent under water bath at 80°C for 15 minutes with a weight ratio of 1:8.8 for use as binder, plasticizer, and dispersant. BT powder Is added to the prepared solution which is then stirred by hand using a glass rod for 5 minutes to achieve uniform dispersion. A small amount of additional DMF is added to the ceramic suspensions to achieve a ratio of 1:8.8. Some of DMF solvent will have evaporated during the water bath and mixing process. The prepared suspension is placed into a 10 mL syringe and piston pushed to the end to remove air inside.

- Initially, a syringe will be used to form a rectangular prism with dimensions of approximately 10 × 10 × 4 mm.

- Using an alumina crucible, the sample will then be sintered in a muffle furnace at various temperatures of 1100, 1200, 1300, and, 1400°C. We will ideally target 1400°C.

- The muffle furnace (a furnace in which the subject material is isolated from the fuel and all of the products of combustion, including gases and flying ash) in SNF or alternatively  at the VQ research facility will be used.

- Eventually, the plan is to use a 3D printer to form the ceramic into a thin film sheet formed on top of the printer heat bed to build a 3D structure for the ceramic suspensions to be deposited onto.

- Amount and form.

  - Approximately 10 g of BaTiO3 powder with particle size <100 nm.

  - Approximately 10 g of PVDF powder.

  - Approximately 20 to 50 mL of DMF in liquid form.

- Storage:

  - The BaTiO3 and PVDF will be stored in the bottles that they were delivered in.

  - The DMF will need to be stored in a solvent cabinet.

- Disposal:

  - The waste DMF and any waste wipes will be disposed in the solvent waste containers in double bagged plastic bags.

To be completed by the PROM COMMITTEE:

Special handling requirements:

On-going approval or staff interaction requirements:

Approved By/Date: